# Combined effect of Laponite and polymer molecular weight on the cell- interactive properties of synthetic PEO-based hydrogels

Arn Mignona,b, Daniele Pezzolib, Emilie Prouvéa, Lucie Lévesqueb, Aysu Arslana, Nele Piena, David Schaubroeckc, Jasper Van Hooricka, Diego Mantovanib, Sandra Van Vlierberghea,⁎,

Peter Dubruela,⁎

a Polymer Chemistry & Biomaterials Research Group, Center of Macromolecular Chemistry, Department of Organic and Macromolecular Chemistry, Ghent University, Krijgslaan 281, Building S4-bis, B-9000 Ghent, Belgium.

b Laboratory for Biomaterials and Bioengineering, CRC-I, Department of Mining, Metallurgical and Materials Engineering and CHU de Quebec Research Centre, Laval University, Pavillon Adrien-Pouliot, 1065 Avenue de la Médecine, Quebec City, QC G1L 3L5, Canada

c Centre of Microsystems Technology (CMST), IMEC and Ghent University, Technologiepark 15, B-9052 Zwijnaarde, Belgium

A R T I C L E I N F O

Keywords:

PEG based Nanoclay Laponite Tunable

Mechanical properties Cell tests

A B S T R A C T

Varying physico-chemical properties of synthetic hydrogels and introducing additives can induce a cell inter- active response of hydrogels. Hydrogels were developed based on acrylate-endcapped urethane-based poly (ethylene glycol) precursors with varying backbone molecular weight (2000–8000 g/mol), in combination with the nanoclay Laponite to explore effects on swelling, mechanical and in vitro biological properties. The com- bined effect of molecular weight and Laponite concentration enables the development of hybrid materials useful for different biomedical applications. Gel fractions approximating 100% along with tunable swelling (4–11 g/g polymer) and mechanical properties (Young's Modulus 0.1–0.6 MPa) are obtained. All materials are non-cyto- toxic and AUPs without Laponite are non cell-interative rendering them suitable for non-adherent biomedical applications. Hydrogels composed of Laponite (0.5 or 1 wt%) and PEG backbone molecular weight of 2000 g/ mol promote cell proliferation useful to function as synthetic dermal matrices or scaffolds for tissue engineering applications.

# Introduction

Polymers are fed into a multitude of biomedical applications (e.g. drug release [1–4], disposable lenses [5,6], tissue engineering [1,7–9] and wound healing [1,10,11]). Synthetic polymers experience however, the disadvantage that they are often non cell-interactive and thus often need to be combined (coated, blended, copolymerized) with natural polymers (such as gelatin or collagen) to enable cell adhesion and subsequent - proliferation [12]. Hydrogel systems have attracted great interest in biotechnological and biomaterial developments because of their high water content, biocompatibility and mechanical properties resembling those of natural tissues [55,56]. Designing a hydrogel platform with appropriate triggers towards regulating cellular behavior through biochemical and biomechanical pathways is increasingly ap- preciated for biomaterials engineering. For example, cellular behavior

can be controlled or guided by simply changing the hydrogel properties. One approach to control cell adhesion is to incorporate adhesive pep- tides such as Arg-Gly-Asp (RGD) that promote cell adhesion through interaction with cell membrane integrins [13]. In another approach to control cellular behavior, Schmidt showed that cell adhesion can be tuned by incorporating gold nanoparticles into soft polymeric films. The gold nanoparticles improved the mechanical properties and in- creased the surface roughness which ultimately contributed to the sti- mulation of cell adhesion. Alternatively, the use of Laponite as physical crosslinker was also reported earlier to promote cell adhesion and - migration onto polymeric hydrogels [14,15].

We hypothesize that by varying the physico-chemical properties of synthetic hydrogels and/or introducing additives, the cell response of hydrogels can effectively be tuned. In the current manuscript, an in- itiator-free, photo-crosslinkable acrylate-endcapped, urethane-based

⁎ Corresponding authors.

E-mail addresses: Arn.Mignon@ugent.be (A. Mignon), Daniele.Pezzoli.1@ulaval.ca (D. Pezzoli), Emilie.Prouve@enscbp.fr (E. Prouvé), lucie.levesque.2@ulaval.ca (L. Lévesque), Aysu.Arslan@ugent.be (A. Arslan), Nele.Pien@ugent.be (N. Pien), David.Schaubroeck@UGent.be (D. Schaubroeck), jasper.vanhoorick@ugent.be (J. Van Hoorick), Diego.Mantovani@gmn.ulaval.ca (D. Mantovani), Sandra.VanVlierberghe@ugent.be (S. Van Vlierberghe), Peter.Dubruel@ugent.be (P. Dubruel).

Acrylate

Spacer

Diiso- cyanate

Backbone (PEG)

Diiso- cyanate

Spacer

Acrylate

Fig. 1.  Structure of acrylate-endcapped, urethane-based poly(ethylene glycol) precursor (m = 6, n depends on the molecular weight of the PEG backbone, x = 1–3).

poly(ethylene glycol) (AUP, Fig. 1) is applied [16]. Photo-crosslinkable hydrogels are of great interest for biomedical applications such as drug delivery and tissue engineering [17,18]. However, one of the main is- sues associated with photo-polymerization is the use of potentially toxic photo-initiators [19,20]. Conversely, the AUP applied herein features a multitude of interesting properties [21]: it can be UV-cured (UV-A) in the absence of a photo-initiator, it shows excellent water solubility (up to 9 g/mL), the crosslinked AUP is biocompatible and the AUP physical properties can be adjusted by varying among other the molecular weight of the polymer backbone [16]. Previous research has shown that urethane moieties enhance the hydrogel flexibility as proven among other by Bacchi et al. [22] and Phan et al. [23] without revealing cell- interactive properties. Poly(urethane)s are therefore often grafted by RGD peptides or coated using biopolymers such as tropoelastin to in- troduce cell adhesion properties [24–26]. Taking into account that the presence of urethane moieties in the AUP precursors is very limited, up to 8 moieties on a theoretical molecular weight ranging between 7500- and 25,500 g/mol (PEG 2k – PEG 8k respectively with a repeating unit of 3), we can safely anticipate that they will have no significant influ- ence on the biological properties (Fig. 1).

In addition to the advantages of the above-mentioned PEG-based AUPs, nanoclays have also shown their potential for tissue engineering purposes, in combination with hydrogels [15,27,28]. Indeed, they can increase the hydrogel strength and improve their in vitro biological response (i.e. cell adhesion and – proliferation) [29]. The nanoparticles can be introduced as fillers entrapped within the network. A well- known nanoclay is Laponite being a synthetic, hydrous magnesium li-

crosslinking efficiency along with swelling experiments. In a sub- sequent part, tensile tests, rheology experiments and stress relaxation assays were performed to determine the mechanical properties of the materials. Next, indirect and direct cell viability tests were executed to assess the in vitro biocompatibility and the cell-interactive properties. Finally, cell adhesion was visualized using fluorescence microscopy.

# Materials and methods

  - Materials

Butylated hydroxytoluene (BHT) was obtained from Innochem GMBH (Wardenburg, Germany). Bismuth neodecanoate (Valikat BI 2010) was purchased from Umicore (Brugge, Belgium). Laponite XLS was received from BYK chemicals. Poly(ethylene glycol) 2000, 4000 and 8000 g/mol, isophorone diisocyanate (IPDI), phenothiazine (PTZ), triphenyl phosphite (TPP) and phosphoric acid were obtained from Sigma-Aldrich (Overijse, Belgium). Gelatin type B was purchased from Rousselot (Gent, Belgium). Bisomer PEA6 was purchased from GEO specialty chemicals (Southampton, UK). Dulbecco's Modified Eagle Medium (DMEM), fetal bovine serum (FBS), phosphate-buffered saline solution (PBS, pH 7.4, 0.1 M) and all other cell culture reagents were obtained from Thermo Fisher Scientific (Waltham, MA, USA), unless stated otherwise.

  - Synthesis of acrylate-endcapped urethane-based poly(ethylene glycol) precusor

0.7

5.5

0.3

8

20

4 0.7

thium silicate (Na+ [(Mg  Li   )Si O  (OH) ]− ) with two tetrahedral

silica sheets sandwiching a central octahedral magnesium sheet [27]. The individual Laponite platelets are characterized by a diameter of

~30 nm and a thickness of ~1 nm [27] while they can form thixotropic gels in water [30]. Due to their structure, the alternating layers of na- noclays resemble the morphology of composite structures found in nature and even human tissue [31,32]. Laponite has already shown its potential towards biomedical applications by releasing Mg2+ ions. The incorporation of Laponite in polymers [33,34] leads to an increased fibroblast cell growth rate and a reduced polymer cytotoxicity. In the present study, Laponite was incorporated as filler within the AUP net- work to introduce cell-interactive properties.

It can thus be hypothesized that the mechanical and the in vitro biological properties of photo-crosslinked synthetic hydrogel networks can be varied by changing the molecular weight of the PEG backbone along with the concentration of the incorporated Laponite. Using this approach, we aim to develop tailor-made hydrogels with potential for biomedical applications for which cell adhesion is either a must (e.g. adipose regeneration [35,36], dermal matrices [37,38]) or undesirable (e.g. wound dressings [1,10,11], resorbable surgical sheets [39]). Pre- vious research by Schmidt et al. [40] has proven that physical inter- actions such as H-bridges exist between Laponite and PEG polymers, which further substantiates our hypothesis that Laponite affects the physico-chemical properties of PEG-based AUP hydrogel films. The AUP hydrogel films were produced with and without Laponite, after which gel fraction experiments were performed to determine the

The synthesis of acrylate-endcapped urethane-based poly(ethylene glycol) (PEG) precursors (AUPs) was previously described by Houben et al. [16,21,41] for a PEG backbone of 2000 g/mol. In the present work, AUPs of varying molecular weight (2000, 4000 and 8000 g/mol) were synthesized. First, PEG (2000, 4000 or 8000 g/mol) was melted with phosphoric acid (173 ppm) at 85 °C in a three-neck flask under mechanical stirring (500 rpm). After the PEG was melted, butylated hydroxytoluene (BHT) was added (500 ppm) as radical scavenger to- gether with 2 equivalents of isophorone diisocyanate (IPDI) for ur- ethanization. Subsequently, the temperature was decreased to 65 °C before adding the bismuth catalyst (Valikat BI 2010, 300 ppm) as the addition of this reagent leads to an exothermal reaction. After 10 min, the system was flushed and kept in a nitrogen environment. Next, the temperature was again increased up to 80 °C and the reaction continued for 2 h. The temperature was then decreased to 65 °C after which 2 equivalents of Bisomer PEA6 was added. The bismuth neodecanoate catalyst was subsequently added (300 ppm) and reaction occurred during 10 min followed by again increasing the temperature to 85 °C. The reaction continued for another 1.5 h in ambient atmosphere. Fi- nally, PTZ and TPP were added as post-stabilizers (500 ppm each). In- frared spectroscopy analysis (PerkinElmer Frontier FT-IR (midIR) combined with a MKII Golden Gate set-up equipped with a diamond crystal from Specac) was performed to confirm the end of the reaction as evidenced by the absence of the N=C=O the IPDI peak at 2260 cm−1 [21] (see Fig. S.1 in Supplementary info).

Table 1

Gel fraction of the AUP polymer networks as a function of the PEG molecular weight and the Laponite concentration.

Network composition	Gel fraction [%]

PEG 2k	98.6 ± 0.3

PEG 2k 0.5% Lap	99.5 ± 0.1

PEG 2k 1% Lap	99.5 ± 0.3

PEG 4k	98.9 ± 0.4

PEG 4k 0.5% Lap	99.5 ± 0.1

PEG 4k 1% Lap	99.1 ± 0.3

fraction could be determined as the ratio of the mass of the dried sample after 24 h incubation over the initial dry mass of the sample. The samples were dried using a Christ freeze-dryer alpha 2–4-LSC.

The swelling capacity was determined on polymer disks with the above mentioned dimensions as the mass change between the dry and the swollen state. Samples were weighted in dry state (wd), followed by incubation in ultrapure water or phosphate buffered saline (PBS) for 3 days. The ratio of the swollen weight, ws and the dry weight results in the swelling capacity according to the following equation:

PEG 8k	97.0 ± 0.5

PEG 8k 0.5% Lap	98.6 ± 0.2

PEG 8k 1% Lap	97.4 ± 0.9

swelling capacity   g

g

= ws	wd

wd

(1)

  - Production of AUP hydrogel films

Hydrogel films were prepared by UV-crosslinking. The AUP were dissolved (30 wt%) in deionized water (PEG 8000 g/mol requires heating up to 40 °C to dissolve) and film casted in rectangular molds (1 mm thickness) on glass plates covered with release foil. Crosslinking for 30 min occurred through UV-A irradiation (25 J/cm2 and a wave- length range of 250–450 nm). For the samples containing Laponite, the same procedure was applied, but Laponite was mixed into the AUP solution at concentrations of 0.5 and 1 wt% prior to film casting and UV crosslinking. The polymers will be further referred to as “PEG xk y% Lap” in which x represents the molecular weight (2, 4 or 8 for 2000, 4000 or 8000 g/mol respectively) and y the weight percentage of Laponite incorporated (0.5 or 1 wt%).

As reference materials for the in vitro cell assays, methacrylamide- modified gelatin (Gel-MOD) was produced. To prepare Gel-MOD sheets (degree of amine group substitution (DS) of 66%), 10 wt% Gel-MOD was dissolved in ultrapure water at 40 °C and the photo-initiator Irgacure®2959 was added to a concentration corresponding to 2 mol% compared to the double bonds present in Gel-MOD [42]. The resulting solution was poured into the same rectangular molds as mentioned above for the AUP, followed by photo-induced crosslinking using UV irradiation (wavelength range of 250–450 nm, 25 J/cm2).

  - Physico-chemical characterization of the polymer networks

By measuring the dry weight of punched polymer disks (14 mm diameter, 1 mm thickness) before and after extraction of the possible leachable fraction in water during 24 h at room temperature, the gel

Scanning electron microscope (SEM) analysis is performed on a JEOL JSM-5600. The apparatus is used in the secondary electron mode (SEI). This SEM apparatus is equipped with an electron microprobe JED 2300 and an EDS (Energy Dispersive Spectroscopy) detector for ele- mental analysis. SEM-EDS is capable of detecting all elements from carbon to uranium, with a detection limit of circa 0.2 wt% for most elements [43]. Prior to analysis, all samples are coated with a thin carbon layer (15–20 nm) via flash evaporation.

The mechanical properties were evaluated by conventional tensile tests, stress relaxation experiments and rheology. Dog bone samples (4 mm wide, 30 mm long in the linear part) were cut from AUP hy- drogel sheets swollen during 24 h in PBS after which the thickness of the samples was evaluated with a scanning laser interferometer (LaserMike 136, Series 183B, NDC Technologies, Dayton, OH, USA). The viscoelastic properties of the developed materials were evaluated by tensile stress-relaxation tests with an Instron ElectroPuls E1000 system (Instron Corporation, Norwood, MA, USA) equipped with a 5 N load cell and controlled by Instron WaveMatrix™ 1.8 software. The samples were pre-swollen at 37 °C in PBS solution overnight. The samples were subsequently mounted into the grips of the mechanical tester and immersed in a bath containing PBS at 37 °C to model pseudo- physiological conditions and to prevent drying. The samples were equilibrated for at least 15 mins in the bath before starting the mea- surements. Five progressive stress-relaxation cycles were applied, con- sisting of 5% strain ramps at 5%/s strain rate followed by a relaxation time of 240 s at constant strain to take into account the viscoelastic behavior of the hydrogels and identify, for each cycle, a steady value for the stress (equilibrium stress). 25% deformation was reached for each sample at the end of the test. The initial elastic Modulus (Emod0) and the elastic equilibrium Modulus (Emodr) were defined by the best fit regression curve of stress-strain relationships for each step immediately

Swelling capacity (g water/g polymer)

Ultrapure water

PBS

14

12

10

8

6

4

2

0

PEG 2k PEG 2k PEG 2k PEG 4k PEG 4k PEG 4k PEG 8k PEG 8k PEG 8k

0.5%

Lap

1% Lap

0.5%

Lap

1% Lap

0.5%

Lap

1% Lap

Fig. 2. Effect of PEG molecular weight and Laponite concentration on the swelling capacity of AUP polymer networks.

ρx (mmol/cm3) (Peppas Merrill)

1.65

0.88

0.33

1.86

0.88

0.36

1.95

0.86

0.35

at the beginning and at the end of the relaxation time respectively. Tensile tests were performed on dog bone samples with the same di- mensions and set-up with a continuous speed of 10 mm/min until break to measure the Young's Modulus and stress at break.

Mc (g/mol) (Peppas Merrill)

680.37

1268.30

3427.22

601.07

1268.30

3127.18

575.06

1299.57

3241.18

ξ (nm) (Peppas- Merrill)

3.13

4.72

9.27

2.89

4.72

8.66

2.81

4.80

8.89

Rheology measurements (Anton Paar Physica MCR 300 rhe- ometer) were performed after overnight swelling in demineralized water. 14 mm diameter, 1 mm thick disks were punched from the swollen samples prior to the test and positioned between the parallel plate set-up of the rheometer. Two different experiments were per- formed in triplicate at a temperature of 37 °C and upon applying a constant force of 1 N to the sample. First, the linear viscoelastic range was determined by increasing the strain from 0.01% to 100% while applying a frequency of 1 Hz. Next, the mechanical spectrum was ob- tained by increasing the frequency from 0.01 to 10 Hz under a constant strain of 0.1%, corresponding to a strain in the linear viscoelastic strain domain of the material determined with the strain scanning test.

To have a better understanding on the mesh pore size and cross- linking density, the rubber elasticity theory was used.

ρx (mmol/cm3) (rubber elasticity theory)

0.49

0.38

0.20

0.47

0.32

0.18

0.47

0.31

0.18

In order to apply the rubber elasticity theory with the aim to de- termine the average molecular weight between crosslinks (Mc), the network chains need to follow the Gaussian statistics model, as re- flected by a linear correlation between log(Q) and log(G) (see Fig. S.2 in Supplementary info) with Q being the volumetric swelling ratio and G the shear modulus which for hydrogel materials can be approximated using the storage modulus (G') as determined via rheology [44,45].

The volumetric swelling ratio can be calculated from the swelling ratio q using the following equation [44,46,47].

(

q

H2O

1

PEGAUP

)

+

(

1

PEGAUP

)

V	1

ξ (nm) (rubber elasticity theory)

5.73

7.22

11.98

5.74

7.85

12.24

5.75

7.99

12.21

v2,s =

p =	=

Vg	Q

(2)

Herein, v2,s corresponds to the polymer volume fraction in the swollen state, while Vp and Vg corresponds to the polymer volume and

the  hydrogel  volume  at  equilibrium  swelling.  ρH2O    and  ρPEGAUP  re- present the density of water (i.e. 1 g/cm3)  and  PEG-based AUP re-

Mc (g/mol) (rubber elasticity theory)

2271.16

2966.93

5714.55

2367.72

3503.96

6248.81

2406.87

3600.36

6112.86

spectively. In the present work, ρPEGAUP was approximated by the density of PEG-diacrylate (PEG-DA, 1.119 g/cm3) [48]. Once the vo- lumetric swelling ratio is known, the average molecular weight be- tween crosslinks can be calculated using the following equation [44,49,50].

cRT Mc

G =	1	2Mc

Mn

1

Q1 3

(3)

( )

V1

Mn (g/mol)

7400

9900

17,800

7400

9900

17,800

7400

9900

17,800

Alternatively, the average mesh size can be calculated purely on the swelling ratio regardless of the mechanical properties using the Peppas- Merril equation: [48].

1	2

| v2.r | (v2.s )1 ( 2.s ) 3 1 v v2.r 2 v2.r |  |
| --- | --- | --- |

v   [ln(1	v2.s) + v2.s +

2

v   ]

1 2.s

Storage modulus (Pa)

72,700

52,367

20,333

66,300

32,333

15,833

63,733

29,233

16,867

Mc = Mn

(4)

Table 2

Overview of the mesh pore size ξ and the cross-link density ρx whereby the average molecular weight between two cross-links (Mc ) can be calculated according to the rubber elasticity theory or the Peppas Merrill theory.

Swelling ratio (q)

Herein, Mn equals the molecular weight of the applied AUP poly- mers, v is the specific volume of the PEG-based AUP which is again approximated by the value for PEG-DA (i.e. 0.893 cm3/g [48]), V1 is the molar volume of the solvent (i.e. 18 cm3/g for water [48]), v2,r is the

4.4

6.2

11.2

4.1

6.2

10.4

4

6.3

10.7

polymer volume fraction in the relaxed state (i.e. 30 wt% or 0.3) and χ1 is the Flory-Huggin's polymer solvent interaction parameter approxi- mated by the value for PEG (i.e. 0.426 for PEG-water [48]).

Sample

PEG 2k PEG 4k PEG 8k

PEG2k 0.5% Lap

PEG 4k 0.5% Lap PEG 8k 0.5% Lap PEG 2k 1% Lap PEG 4k 1% Lap PEG 8k 1% Lap

As the swelling potential is especially taken into account, the cal- culations done for Peppas-Merrill are more relevant for polymers. However, the mechanical properties are not included for the calcula- tions, which are taken into account with the rubber elasticity theory.

Once the average molecular weight between the crosslinks is cal- culated, the mesh size (ξ) of the hydrogel can be calculated using the

Fig. 3. SEM-EDS (secondary electron mode) measurement of PEG 2k 1% Lap with the SEM image (top left) and the EDS identifying the presence of respectively C, O, Si and Mg.

Table 3

Mass percentage distribution of AUP hydrogels measured by SEM-EDS.

Where l is the carbon-carbon bond length (i.e. 0.154 nm), Cn is the Flory characteristic of the polymer, herein approximated by the char-

Element      PEG 2k     PEG 2k 0.5%

Lap

PEG 2k 1%

Lap

PEG 8k     PEG 8k 1%

Lap

acteristic parameter for PEG (i.e. 4.1) [52]. Mr is the molecular weight of one repeating unit, again approximated by using PEG as reference

(i.e. 2 carbons, 4 hydrogens and 1 oxygen = 44 g/mol). Once the

Mass%       Mass%	Mass%	Mass%       Mass%

C	73.1	68.5	72.3	77.8	76.7

O	26.7	30.2	24.9	22.2	21.0

Mg	< DL	0.5	1.1	< DL	0.8

Si	< DL	0.9	1.7	< DL	1.5

Total	100	100	100	100	100

DL stands for detection limit.

90

80	PEG 2k 0.5% Lap

Storage Modulus (kPa)

70

60	PEG 4k 0.5% Lap

50	PEG 8k 0.5% Lap

40

30

20

10

0

0.01	0.1	1	10	100

Strain (%)

average molecular weight between crosslinks (Mc ) and the specific volume of the polymer (v) is known (i.e. approximated by the specific volume of PEGDA being 0.893 cm3/g [48]), the crosslink density ρx can be calculated using the following equation [44,47].

Mc

x =   1	(7)

  - Cell culture and cell tests

Primary Neonatal Human Dermal Fibroblasts (HDFs, Gibco C0045C, Thermo Fisher Scientific) were cultured in DMEM supplemented with 100 U mL−1 penicillin, 0.1 mg mL−1 streptomycin and 10% FBS, here- after referred to as complete medium.

Indirect cytotoxicity tests were performed according to ISO 10993-5 aiming to investigate whether or not cytotoxic products are released from the samples after the sterilization and purification process, as previously reported [53]. After the preparation, polymer sheets were incubated and swollen overnight (o.n.) at room temperature (r.t.) in PBS supplemented with 100 U mL−1 penicillin and 0.1 mg mL−1 streptomycin. Then, round samples (diameter = 15.6 mm,   thick- ness = 1 mm), finely fitting the dimensions of the wells of 24-well

Fig. 4. Effect of PEG molecular weight on the storage modulus by a strain scan obtained via rheology by increasing the strain from 0.01% to 100% while ap- plying a frequency of 1 Hz.

following equation [51].

plates, were punched from swollen polymer sheets and incubated for 24 h in ethanol (EtOH) for sterilization. The samples were washed 4 times during 24 h in sterile PBS for purification to completely remove unreacted and side products of the photo-crosslinking step. The mate- rials were then incubated in 1 mL of complete medium at 37 °C and

2

1

= (r0) 2 v

1

3

2.s

(5)

extraction medium was harvested after 24 h. HDFs were seeded at a

density of 1.5 × 104 cells cm−2 in 96-well plates. After 24 h, the culture medium was removed and replaced with 100 μL of material extracts or

0

where (r2) is the root mean square end-to-end distance of the polymer in

0

its free state:

complete DMEM, as positive control. Cell viability was evaluated 24 h later by an AlamarBlue assay. Briefly, materials extracts or complete

(r2) = l2

2 Mc  C

n

Mr

(6)

medium were replaced with 100 μL of complete medium containing 10% of 1× resazurin dye and incubated at 37 °C for 2 h. The fluores- cence of the medium was measured (λex = 560 nm; λem = 590 nm)

Fig. 5. Effect of PEG molecular weight and Laponite concentration on the storage modulus. Rheology experiments show the storage modulus as a function of the frequency while applying a constant strain of 0.1% comparing PEG 2k, PEG 4k and PEG 8k and PEG 2k without Laponite (left) versus PEG 2k supplemented with 0.5 and 1 wt% Laponite (right).

0.7

Young's Modulus [MPa]

0.6

0.5

0.4

0.3

0.2

0.1

0

PEG 2k	PEG 2k

0.5% lap

PEG 2k 1%

lap

PEG 4k	PEG 4k

0.5% lap

PEG 4k 1%

lap

PEG 8k	PEG 8k

  - % lap

PEG 8k 1%

lap

Fig. 6. Effect of PEG molecular weight and Laponite concentration on Young's Modulus of the crosslinked AUP polymers as obtained from the stress-strain plots obtained via tensile tests.

Stress at break [MPa]

0.6

0.5

0.4

0.3

0.2

0.1

0

PEG 2k 0.5% PEG 4k 0.5% PEG 8k 0.5%

0.6

Stress at break [MPa]

0.5

0.4

0.3

0.2

0.1

0

PEG 2k	PEG 2k 0.5%

PEG 2k 1%

lap

lap

lap

lap

lap

Fig. 7. Stress at break of the crosslinked AUP polymers as derived from tensile testing. The left panel shows the effect of the PEG molecular weight on the stress at break of 0.5 wt% Laponite-containing hydrogels. The right panel shows the effect of an increasing Laponite concentration on the stress at break for PEG 2k AUPs.

using a multi-mode microplate reader system SpectraMax i3x (Mole- cular Devices, Sunnyvale, CA, USA) and the viability was evaluated with respect to the fluorescence of the control cells.

Cell adhesion and proliferation on the developed materials were in- vestigated by directly seeding HDFs on the surface of the samples. Samples were seeded with 1 × 104 cells cm−2 in complete DMEM without phenol red (Thermo Fisher Scientific) and incubated in a cell culture incubator at 37 °C. 24 h, 72 h and 7 days after seeding, the medium was replaced with 1 mL of complete DMEM without phenol red supplemented with 0.5 mg mL−1 MTT (Sigma Aldrich) and incubated

for 4 h in a cell culture incubator. Then, the samples were incubated in 500 μL of dimethyl sulfoxide (DMSO) and placed on an orbital shaker at

r.t. for 30 mins to dissolve the formed formazan crystals. The absor- bance at 570 nm of 200 μL of the resulting solution was finally mea- sured in transparent 96-well plates. Samples without cells served as controls.

Cell staining. Samples were stained with Phalloidin-TRITC (Sigma Aldrich) and DAPI (Sigma Aldrich) to visualize the actin filaments and the nuclei of the cells respectively. Briefly, the samples were washed with PBS and fixed with 3.7% formaldehyde (Sigma) for 2 h. Next, the

Fig. 8. Plots resulting from stress relaxation tests performed on AUP PEG 2k as representative example for the crosslinked AUPs.

cells were permeabilized with 0.1% Triton X-100 in PBS for 30 min at r.t., incubated for 1 h at r.t. in the dark with Phalloidin-TRITC and DAPI in PBS and finally washed three times with PBS. Images were acquired with an Olympus BX51 fluorescence microscope.

# Results and discussion

In the present work, we aim to explore the effect of varying the molecular weight of the PEG backbone along with the concentration of the incorporated Laponite on the mechanical and the in vitro biological properties of photo-crosslinked synthetic hydrogel networks.

To this end, in this work, acrylate-endcapped urethane-based poly (ethylene glycol) (PEG) precursors with different PEG molecular weight were photo-crosslinked under photo-initiator-free UV-A conditions. The nanoclay Laponite was introduced prior to crosslinking to evaluate its effect on the mechanical and the in vitro biological properties of the developed biomaterials. A PEG precursor concentration of 30 wt% was selected throughout our work as previous reports from our research group showed that 30 wt% AUP films resulted in a Young's Modulus of

  - MPa [21]. The latter is in agreement with the mechanical properties required for a multitude of biomedical applications including contact lenses, as well as tissue engineering substrates (articular cartilage, aorta, bladder…) [54–56]. As an example, the MW distribution of PEG 2k has been included in the Supplementary info [57].

  - Physico-chemical characterization of the crosslinked hydrogels

To determine the crosslinking efficiency of the photo-crosslinked hydrogels, first the gel fraction was evaluated. As indicated in Table 1, the gel fraction of all AUP polymers was close to 100% (> 97%) re- vealing a high curing efficiency. The addition of Laponite had no ad- verse effect on the crosslinking process of the AUP polymers in the applied concentration range. The obtained gel fraction values are very promising, especially when compared to earlier reported PEG diacry- late-based systems which demonstrated gel fraction values ranging between 50 and 85% [58,59] (Table 1).

Table 4

Upon increasing the molecular weight of the AUP backbone, the hydrogel swelling increased, as anticipated (Fig. 2). In fact, an increase of the molecular weight results in a lower number of crosslinking points which is accompanied with a higher amount of absorbed water. To gain further insight in the hydrogels' physical properties including the mesh pore size and the cross-linking density, the rubber elasticity theory and the theory established by Peppas Merrill were implemented using Eqs. (2)–(7) (Table 2).

As anticipated, an increase in MW (for PEG 2k to PEG8k) resulted in a larger average pore size and a decrease in cross-link density (i.e.

5.7 nm and 0.49 mmol/cm3 versus 7.2 nm and 0.38 mmol/cm3 for PEG

2k and PEG 8k respectively) for the crosslinked hydrogels. Interestingly, the results showed that addition of Laponite at different MW only exerted a limited effect on both pore size and cross-link density.

The comparison between swelling capacities in ultrapure water and PBS revealed similar swelling behaviors, although PBS buffer lead to a small but significant (p < .05) buffer ion mediated decrease in swelling [60,61] (Fig. 2, Table 2).

To identify the distribution of Laponite inside the AUP hydrogels, SEM-EDS measurements have been performed. This was done on PEG 2k, PEG 2k 0.5% Lap, PEG 2k 1% Lap, PEG 8k and PEG 8k 1% Lap to compare the effect of MW of PEG and the percentage of Laponite. SEM indicates the smooth surface of the AUP, even with additional Laponite (See Fig. 3 and Supplementary info Figs. S.4–S.7). EDS has shown the homogeneous distribution of Laponite (H12Li2Mg16Na2O72Si24) on the AUP surface by the elemental analysis of Si and Mg (see also Fig. 3 and Supplementary info Figs. S.4–S.7). The mass percentage distribution for all samples is described in Table 3. The mass percentage of Mg and Si in the samples without Laponite (PEG 2k and PEG 8k) are below the de- tection limit (DL), indicating that only background is measured, as expected [43]. As anticipated, the presence of Mg and Si is about half in PEG 2k 0.5% Lap compared to PEG 2k 1% Lap. The SEM-EDS thus enables to show the presence of as well as the homogeneous distribu- tion of Laponite on the AUP hydrogel surface (Fig. 3, Table 3).

  - Mechanical characterization of the crosslinked AUP hydrogels

    - Storage modulus determination through rheology

Rheology is a sensitive technique often used to characterize the mechanical properties of hydrogels as minor structural changes often result in a different rheological response. Due to the Winter-Chambon criterion (convergence of the loss tangent at the gel point), only G' is plotted for the rheology measurements [62]. A strain of 0.1% was se- lected for the rheological experiments based on the linear viscoelastic strain domain as identified in Fig. 4 and as described in the Materials & Methods section. This value was selected for all samples in order to record a mechanical spectrum between 0.01 and 10 Hz (Fig. 4).

Rheology experiments showed that an increase of the backbone molecular weight induced a decrease in storage Modulus (Fig. 5, left panel) what is related to the lower crosslinking density of the resulting networks for the higher PEG molecular weight. Conversely, the addition

Emod0, Emodr, Young's Modulus (from tensile tests) and Emodr/Emod0 ratio expressed as elastic percentage of the AUP polymers, evaluated by stress relaxation tests.

| Network composition | Emod0 [MPa] | Emodr [MPa] | Young's modulus [MPa] | Elastic percentage [%] |
| --- | --- | --- | --- | --- |
| PEG 2k | 0.49 ± 0.03 | 0.46 ± 0.03 | 0.58 ± 0.02 | 96 ± 1 |

PEG 2k 0.5% Lap	0.40 ± 0.05	0.39 ± 0.03	0.61 ± 0.03	95 ± 2

PEG 2k 1% Lap	0.53 ± 0.01	0.50 ± 0.01	0.43 ± 0.02	97 ± 1

PEG 4k	0.25 ± 0.03	0.24 ± 0.02	0.22 ± 0.02	95 ± 1

PEG 4k 0.5% Lap	0.29 ± 0.02	0.28 ± 0.02	0.29 ± 0.03	92 ± 3

PEG 4k 1% Lap	0.23 ± 0.01	0.22 ± 0.01	0.29 ± 0.02	95 ± 0

PEG 8k	0.08 ± 0.01	0.07 ± 0.01	0.12 ± 0.03	92 ± 3

PEG 8k 0.5% Lap	0.08 ± 0.00	0.08 ± 0.00	0.09 ± 0.01	92 ± 1

PEG 8k 1% Lap	0.05 ± 0.01	0.05 ± 0.01	0.13 ± 0.01	85 ± 7

1 day

3 days

7 days

PEG 2k    PEG 4k    PEG 8k    PEG 2k    PEG 4k    PEG 8k    PEG 2k    PEG 4k    PEG 8k

0.5% lap 0.5% lap 0.5% lap 1% lap    1% lap    1% lap

80	Fig. 9. Effect of PEG molecular weight and Laponite con-

centration on nHDF adhesion and proliferation as studied by

Cell adhesion compared to Gel-MOD (%)

70	direct cytotoxicity tests. The results are expressed as per-

centage cell adhesion  as compared to  Gel-MOD as positive

60	control. The result at day 1 provide an indication of the cell

adhesion while the data after 3 and 7 days give insight in the

50	initial cell proliferation onto the hydrogels.

40

30

20

10

0

-10

of Laponite only minimally influences the storage Modulus (Fig. 5, right panel). The latter was also observed previously by Lapasin et al. [63] who monitored the effect of Laponite on the Modulus of scleroglucan hydrogels. All hydrogels displayed a high degree of elasticity with G' being only negligibly dependent on the frequency as was also found in literature for PLLA-PEO-PLLA tri-block copolymer hydrogels [64] (Fig. 5).

    - Young's Modulus and stress at break determination through tensile tests

Tensile tests indicated that an increase in the PEG molecular weight corresponded with a decrease in the Young's Modulus, both in the presence and in the absence of Laponite (Fig. 6). An example of a stress- strain curve was added in Supplementary info (Fig. S.8). The latter is again reasonable as a shorter chain length goes together with a higher amount of crosslinks (see cross-linking density in Table 2), a network with a lower swelling capacity (see §3.1) and thus a higher stiffness [65].

On the other hand, the presence of Laponite into the crosslinked AUPs seems to exert different effects depending on the AUP molecular weight applied. The latter can be explained by two different factors including the distribution of the Laponite nanoparticles (100 nm) within the crosslinked network as well as the shear thinning behavior of Laponite [63,66]. For PEG 4k, the addition of Laponite increases the strength of the crosslinked polymer as evidenced by the significant increase in the Young's Modulus (p < .05) upon addition of the na- noclay. For the PEG 2k and PEG 8k, a similar effect was anticipated. For the PEG 8k, however, the effect on the strength only became apparent for higher Laponite concentrations (i.e. 1 wt% versus 0.5 wt%). In contrast to the expectations, the effect of Laponite on the Young's Modulus on PEG 2k networks reveals a different trend. The latter is not resulting from a change in the cross-link density nor the pore-size as these changes are only minor upon increasing the Laponite concentra- tion (see Table 2). This can be explained by the higher network density as compared to the higher PEG molecular weight counterparts. As a result, another effect should be considered. Addition of nanocrystals within a dense network could increase the shear thinning effect of La- ponite in the crosslinked network thereby resulting in a decrease of the Young's Modulus as observed earlier by Pei et al. [67]. The reinforcing effect of Laponite is thus counteracted by an increasing shear thinning behavior which occurs above a critical Laponite concentration de- pending on the polymer molecular weight applied (Fig. 6).

Next, the stress at break values were also investigated and similar trends as observed for the Young's Modulus were obtained. Upon in- creasing the molecular weight of the AUP backbone, a decrease in stress

at break was observed (Fig. 7 (left)) albeit not significant in the absence of Laponite and upon 1 wt% addition of Laponite, data not shown). Similar as the Young's Modulus results, an increase of the Laponite concentration for the PEG 2k polymers first resulted in a non-significant (p > 0.05) increase of the stress followed by a significant decrease upon incorporation of 1 wt% nanoclay as visualized in Fig. 7 (right). A similar trend was found for the PEG 4k polymers. For the PEG 8k polymers, a non-significant increase was observed for the 0.5 wt% na- noclay concentration while a significant increase in stress at break could be observed when 1 wt% Laponite was incorporated (data not shown) (Fig. 7).

    - Stress relaxation determination

Given that a visco-elastic behavior is often observed for hydrogels and hydrogel composites [68], progressive tensile stress relaxation tests were performed on the AUPs as shown in Fig. 8. Particularly, the initial elastic Modulus (Emod0) and the equilibrium (relaxed) elastic Modulus (Emodr) were analyzed and the Emodr/Emod0 ratio was calculated as an index of the elastic contribution in the visco-elastic behavior of the crosslinked hydrogels [69,70] (Table 4). For all materials, a constant behavior was observed for all stress-relaxation cycles, with a rapid, yet limited decrease of the stress followed by a plateau. Interestingly, the Emodr/Emod0 ratio was extremely high, with values exceeding 90% for all materials except for PEG 8k 1 wt% Lap, which reached 85%, thereby demonstrating an almost completely elastic behavior. This strongly elastic behavior confirms what was also observed by rheology mea- surements. Addition of Laponite did not lead in any case to a significant decrease of the elastic percentage. It is worth highlighting that for certain applications such as wound dressings on elbows, heels or knees, the currently available materials cannot rapidly adapt to the deforma- tions occurring at the site of the injury which often causes detachment. Therefore, the materials developed herein could offer a major ad- vantage as they show elastic behavior exceeding 95% (Table 4, Fig. 8).

  - In vitro biocompatibility assessment

In a final part of the research, the cytocompatibility of the devel- oped hydrogels was evaluated by indirect cytotoxicity tests using pri- mary neonatal human dermal fibroblasts (nHDF). The results of all materials tested indicated no significant cytotoxicity for any of the materials tested (viability ≥100% with respect to the control, see supplementary info, Table S.1). The data are in agreement with pre- vious reports describing the cytocompatibility of PEG-based materials [21,71], PEG diacrylates [18] and Laponite [15].

Next, cell-material interactions were evaluated by cell adhesion and

Fig. 10. Effect of PEG molecular weight and Laponite (1 wt%) concentration on nHDF adhesion as studied by fluorescence microscopy of the cell-seeded samples (nHDF) by direct cytotoxicity tests during 1 (left), 3 (center) and 7 (right) days.

proliferation assays using nHDF (Fig. 9). The cells were seeded onto the AUP hydrogels and the cell adhesion was evaluated after 1, 3 and 7 days. Hydrogels based on photo-crosslinked methacrylamide-mod- ified gelatin (Gel-MOD) were used as positive control since these ma- terials are recognized for their excellent cell-adhesive properties [72–75] while they are also used as (commercial) bioinks [76]. As anticipated, based on the AUP backbone being PEG, the materials without Laponite showed almost no cell adhesion nor - proliferation, even after 7 days [77]. Interestingly, the incorporation of Laponite led to a significant increase of the cell adhesion and proliferation in a La- ponite concentration and AUP molecular weight dependent manner. For PEG 2k, the addition of 1 wt% Laponite led to a strong increase in cell adhesion and –proliferation (cell adhesion levels of 60% compared

to Gel-MOD). This effect decreases with an increasing PEG MW. Indeed, for PEG 8k, no cell adhesion was observed, even for the 1 wt% Laponite condition. These data thus indicate the possibility to change cell-ad- hesion properties of developed AUP hydrogels by modifying the Lapo- nite concentration and/or the polymer backbone molecular weight. Brafman et al. have shown that an increase of the molecular weight of a polymer above a certain value decreases the cell attachment [78]. In addition, Kutty et al. already studied the effect of the molecular weight of hyaluronic acid incorporated into PEG-diacrylate-based semi-inter- penetrating networks on the cell response [79]. They observed that there is an inverse relationship between nHDF cell adhesion and the molecular weight applied. It should be noted that in the current manuscript the MW between the crosslinkable functionalities was

varied in contrast with the paper from Kutty et al. It was already in- dicated earlier in literature that Laponite nanoparticles provide a high surface area for protein binding, as well as a high surface energy that favors electron transfer between Laponite and the protein [15,80]. EDX measurements have shown the Laponite concentrations at the surface for the different AUP polymers (Table 3). In addition, the Laponite is homogeneously distributed over the hydrogel surfaces (Figs. S.4–S.7). Due to the swelling differences between PEG 2k and PEG 8k (Fig. 2), it is anticipated that the Laponite density for PEG 8k is lower on the hydrogel surface, resulting in inferior cell adhesion.

As discussed earlier by Gaharwar et al., divalent cations play a significant role in cell adhesion onto biomaterial surfaces [15]. In ad- dition, material properties such as hydration and mechanical properties also strongly influence the cell response. Indeed, Gaharwar et al. showed that an increase of the Laponite concentration resulted in im- proved mechanical properties and superior cell adhesion of osteoblasts. The latter indicates that Laponite also exhibits a significant effect on other cell types than Primary Neonatal Human Dermal Fibroblasts. However, the concentrations used in that paper are higher compared to what was applied in the current manuscript (~40–70% higher). They also reported that, as anticipated, PEG-based polymers did not result in cell adhesion.

As described in Section 3.1 the pore size of the different hydrogels ranges between 3 and 12 nm (Table 2). This size difference is not an- ticipated to cause a difference in cell proliferation as the fibroblasts are in the range of 10–15 μm [81]. Based on the conclusions within the Laponite concentration and AUP MW range studied, a concentration of 1% Laponite combined with a low molecular weight AUP (i.e. 2000 g/ mol) resulted in the best cell adhesion and - proliferation. To further pave the way towards novel applications, possibly lower MW AUP's combined with higher Laponite concentrations could be evaluated in future research.

The results obtained in the cell adhesion studies were confirmed by fluorescence microscopy of the cell-seeded samples, showing almost no cells on AUP hydrogels without Laponite while cells adhered and pro- liferated on hydrogel surfaces containing Laponite, in particular for PEG 2k and to a lesser extent for PEG 4k. However, for PEG 8k con- taining 1 wt% Laponite, almost no cell adhesion and - proliferation was observed (see Fig. 10 and Supplementary info: Figs. S.9–S.11). As such, the synergetic effect of Laponite and a variation of the PEG molecular weight indeed leads to a tunable cell adhesion.

Altogether, the cell tests demonstrated that the developed AUP- based hydrogels are non-cytotoxic and that their interaction with cells can be easily modulated by addition of Laponite while appropriately selecting the backbone molecular weight. Interestingly, the AUPs re- sistant to cell adhesion (e.g. AUPs without Laponite) could be applied for non-adherent wound dressings for which the attachment of cells and the growth of new tissue onto/within the dressing is not desired be- cause of the need for easy removal without trauma [82]. Conversely, AUP hydrogels which promote cell attachment and - proliferation (characterized by 1% Laponite and low PEG molecular weight of 2000 g/mol) could be useful as synthetic dermal replacements or for tissue engineering applications, for which they should provide a sup- port for cell colonization thereby stimulating tissue regeneration [83,84]. To a lesser extent, PEG 2k with 0.5% Laponite and PEG 4k with 1% Laponite also show cell adhesion properties (cell adhesion levels of 22 and 26% compared to Gel-MOD respectively) (Figs. 9 and 10).

# Conclusions

In this study, acrylate-endcapped urethane-based poly(ethylene glycol) polymer precursors combined with the nanoclay Laponite were developed to change their cell response. A series of materials with a wide range of mechanical and biological properties were thus obtained. The crosslinked polymers are characterized by high gel fractions close to 100% and are associated with tunable swelling properties depending

on the molecular weight of the PEG backbone. The addition of Laponite induced a small but significant reduction of the swelling capacity, especially for PEG 8k. The photo-crosslinked AUPs resulted in materials with Young's Modulus ranging from 0.1 up to 0.6 MPa. Additionally, the mechanical properties can also be improved by varying the PEG mo- lecular weight and by incorporation of Laponite. Interestingly, all ma- terials have an elastic percentage around 95%. The cell tests indicated that all materials are non-cytotoxic and that AUPs without Laponite are resistant to cell adhesion and thus suitable for non-adherent applica- tions such as wound dressings or resorbable surgical sheets, while hy- drogels with a concentration of Laponite (1%) combined with low PEG molecular weight (2k) promote cell attachment and - proliferation (up to 60% compared to Gel-MOD) and could be useful as synthetic dermal replacement or scaffolds for tissue engineering applications, for which they would provide an adequate environment supporting cell coloni- zation and tissue regeneration. To a lesser extent, PEG 2k with 0.5% Laponite and PEG 4k with 1% Laponite also show cell adhesion prop- erties (cell adhesion levels of 22 and 26% compared to Gel-MOD re- spectively). Addition of Laponite and varying the molecular weight of the PEG backbone thus leads to hydrogels with tunable mechanical and cell adhesive properties. The usefulness of Laponite in combination with these AUPs can be further exploited as antibacterial agent since Laponite has already proven to be useful as antibiotic eluting clay for wound healing purposes [33].

# Acknowledgements

This project has received funding from the Interreg 2 Seas pro- gramme 2014–2020 co-funded by the European Regional Development Fund under subsidy contract No 2S01-027. This work has also received funding from Research Foundation Flanders (Co-extrusion electrospin- ning as novel tool for the next generation wound dressings: taking ul- timate control over the dressing mechanical and release properties. No. 12Z2918N and Developing an in vitro model of the vascular wall al- ternative to in vivo tests by promoting elastin production in cellu- larised-collagen-based nanofibrous scaffolds G0F0516N).

# Appendix A. Supplementary data

Supplementary data to this article can be found online at https:// doi.org/10.1016/j.reactfunctpolym.2018.12.017.

# References

- E. Caló, V.V. Khutoryanskiy, Biomedical applications of hydrogels: a review of patents and commercial products, Eur. Polym. J. 65 (2015) 252–267.

- A. Pourjavadi, S. Barzegar, Synthesis and evaluation of pH and thermosensitive pectin-based superabsorbent hydrogel for oral drug delivery systems, Starch - Stärke 61 (3–4) (2009) 161–172.

- M. Torres-Lugo, N.A. Peppas, Molecular design and in vitro studies of novel pH-

sensitive hydrogels for the oral delivery of calcitonin, Macromolecules 32 (20) (1999) 6646–6651.

- Y. Wang, J. Wang, Z. Yuan, H. Han, T. Li, L. Li, X. Guo, Chitosan cross-linked poly (acrylic acid) hydrogels: drug release control and mechanism, Colloids Surf. B:

Biointerfaces 152 (2017) 252–259.

- H. Thissen, T. Gengenbach, R. du Toit, D.F. Sweeney, P. Kingshott, H.J. Griesser,

L. Meagher, Clinical observations of biofouling on PEO coated silicone hydrogel contact lenses, Biomaterials 31 (21) (2010) 5510–5519.

- V. Franklin, M. Broadbent, A. Panaser, B. Tighe, Effects of daily disposable silicone

hydrogel lenses on the tear film lipid layer, Contact Lens Anterior Eye 38 (2015) e29.

- T.K. Giri, A. Thakur, A. Alexander, H. Badwaik, D.K. Tripathi, Modified chitosan

hydrogels as drug delivery and tissue engineering systems: present status and ap- plications, Acta Pharm. Sin. B 2 (5) (2012) 439–449.

- M. Maisani, D. Pezzoli, O. Chassande, D. Mantovani, Cellularizing hydrogel-based scaffolds to repair bone tissue: how to create a physiologically relevant micro-en-

vironment? J. Tissue Eng. 8 (2017) (2041731417712073).

- C. Loy, S. Meghezi, L. Lévesque, D. Pezzoli, H. Kumra, D. Reinhardt,

J.N. Kizhakkedathu, D. Mantovani, A planar model of the vessel wall from cellu-

larized-collagen scaffolds: focus on cell–matrix interactions in mono-, bi-and tri- culture models, Biomater. Sci. 5 (1) (2017) 153–162.

- D.W. Kim, K.S. Kim, Y.G. Seo, B.-J. Lee, Y.J. Park, Y.S. Youn, J.O. Kim, C.S. Yong,

S.G. Jin, H.-G. Choi, Novel sodium fusidate-loaded film-forming hydrogel with easy application and excellent wound healing, Int. J. Pharm. 495 (1) (2015) 67–74.

- M. Sadeghi, H. Hosseinzadeh, Synthesis of starch—poly(Sodium Acrylate-co- Acrylamide) superabsorbent hydrogel with salt and pH-responsiveness properties as

a drug delivery system, J. Bioact. Compat. Polym. 23 (4) (2008) 381–404.

- M. Dash, F. Chiellini, R. Ottenbrite, E. Chiellini, Chitosan—a versatile semi-syn- thetic polymer in biomedical applications, Prog. Polym. Sci. 36 (8) (2011) 981–1014.

- D. Pezzoli, P. Tarsini, L. Melone, G. Candiani, RGD-derivatized PEI-PEG copoly-

mers: influence of the degree of substitution on the targeting behavior, J. Drug Del. Sci. Technol. 37 (2017) 115–122 Supplement C.

- K. Haraguchi, T. Takehisa, M. Ebato, Control of cell cultivation and cell sheet de-

tachment on the surface of polymer/clay nanocomposite hydrogels, Biomacromolecules 7 (11) (2006) 3267–3275.

- A.K. Gaharwar, P.J. Schexnailder, B.P. Kline, G. Schmidt, Assessment of using

Laponite® cross-linked poly(ethylene oxide) for controlled cell adhesion and mi- neralization, Acta Biomater. 7 (2) (2011) 568–577.

- A. Houben, P. Roose, H. Van den Bergen, H. Declercq, J. Van Hoorick, P. Gruber,

A. Ovsianikov, D. Bontinck, S. Van Vlierberghe, P. Dubruel, Flexible oligomer

spacers as the key to solid-state photopolymerization of hydrogel precursors, Mater. Today Chem. 4 (2017) 84–89.

- S. Sant, S.L. Tao, O.Z. Fisher, Q. Xu, N.A. Peppas, A. Khademhosseini, Microfabrication technologies for oral drug delivery, Adv. Drug Deliv. Rev. 64 (6)

(2012) 496–507.

- K.T. Nguyen, J.L. West, Photopolymerizable hydrogels for tissue engineering ap- plications, Biomaterials 23 (22) (2002) 4307–4314.

- A.S. Hoffman, Stimuli-responsive polymers: biomedical applications and challenges for clinical translation, Adv. Drug Deliv. Rev. 65 (1) (2013) 10–16.

- C.G. Williams, A.N. Malik, T.K. Kim, P.N. Manson, J.H. Elisseeff, Variable cyto- compatibility of six cell lines with photoinitiators used for polymerizing hydrogels

and cell encapsulation, Biomaterials 26 (11) (2005) 1211–1218.

- A. Houben, N. Pien, X. Lu, F. Bisi, J. Hoorick, M.N. Boone, P. Roose, H. Bergen,

D. Bontinck, T. Bowden, Indirect solid freeform fabrication of an initiator-free

photocrosslinkable hydrogel precursor for the creation of porous scaffolds, Macromol. Biosci. 16 (12) (2016) 1883–1894.

- A. Bacchi, C.S. Pfeifer, Rheological and mechanical properties and interfacial stress

development of composite cements modified with thio-urethane oligomers, Dent. Mater. 32 (8) (2016) 978–986.

- A.C. Phan, M.-l. Tang, J.-F. Nguyen, N.D. Ruse, M. Sadoun, High-temperature high- pressure polymerized urethane dimethacrylate—mechanical properties and

monomer release, Dent. Mater. 30(3) (2014) 350–356.

- H.-B. Lin, S.L. Cooper, Synthesis, Surface and Cell-adhesion Properties of Polyurethanes Containing Covalently Grafted RGD-Peptides, MRS Online

Proceedings Library Archive 331 (1993).

- S.-H.S.-h. Hsu, W.-C. Chen, Improved cell adhesion by plasma-induced grafting of L- lactide onto polyurethane surface, Biomaterials 21 (4) (2000) 359–367.

- D.V. Bax, A. Kondyurin, A. Waterhouse, D.R. McKenzie, A.S. Weiss, M.M. Bilek,

Surface plasma modification and tropoelastin coating of a polyurethane co-polymer

for enhanced cell attachment and reduced thrombogenicity, Biomaterials 35 (25) (2014) 6797–6809.

- X. Tang, S. Alavi, Structure and physical properties of starch/poly vinyl alcohol/ laponite RD nanocomposite films, J. Agric. Food Chem. 60 (8) (2012) 1954–1962.

- M. Miyazaki, T. Maeda, K. Hirashima, N. Kurokawa, K. Nagahama, A. Hotta, PEG-

based nanocomposite hydrogel: thermoresponsive sol-gel transition controlled by PLGA-PEG-PLGA molecular weight and solute concentration, Polymer 115 (2017)

246–254.

- A.K. Gaharwar, C. Rivera, C.-J. Wu, B.K. Chan, G. Schmidt, Photocrosslinked na-

nocomposite hydrogels from PEG and silica nanospheres: structural, mechanical and cell adhesion characteristics, Mater. Sci. Eng. C 33 (3) (2013) 1800–1807.

- T.U. Patro, H.D. Wagner, Layer-by-layer assembled PVA/Laponite multilayer free-

standing films and their mechanical and thermal properties, Nanotechnology 22 (45) (2011) 455706.

- G. Nitya, G.T. Nair, U. Mony, K.P. Chennazhi, S.V. Nair, In vitro evaluation of electrospun PCL/nanoclay composite scaffold for bone tissue engineering, J. Mater.

Sci. Mater. Med. 23 (7) (2012) 1749–1761.

- A.H. Ambre, K.S. Katti, D.R. Katti, Nanoclay based composite scaffolds for bone tissue engineering applications, J. Nanotechnol. Eng. Med. 1 (3) (2010) 031013.

- M. Ghadiri, W. Chrzanowski, R. Rohanizadeh, Antibiotic eluting clay mineral

(Laponite®) for wound healing application: an in vitro study, J. Mater. Sci. Mater. Med. 25 (11) (2014) 2513–2526.

- L. Pachuau, Recent developments in novel drug delivery systems for wound healing,

Expert Opin. Drug Deliv. 12 (12) (2015) 1895–1909.

- Y.S. Chun, K. Verma, H. Rosen, S. Lipsitz, D. Morris, P. Kenney, E. Eriksson, Implant-based breast reconstruction using acellular dermal matrix and the risk of

postoperative complications, Plast. Reconstr. Surg. 125 (2) (2010) 429–436.

- A.S. Liu, H.-K. Kao, R.G. Reish, C.A. Hergrueter, J.W. May Jr, L. Guo, Postoperative complications in prosthesis-based breast reconstruction using acellular dermal matrix, Plast. Reconstr. Surg. 127(5) (2011) 1755–1762.

- S.-P. Huang, C.-C. Hsu, S.-C. Chang, C.-H. Wang, S.-C. Deng, N.-T. Dai, T.-M. Chen,

J.Y.-H. Chan, S.-G. Chen, S.-M. Huang, Adipose-derived stem cells seeded on acel- lular dermal matrix grafts enhance wound healing in a murine model of a full-

thickness defect, Ann. Plast. Surg. 69 (6) (2012) 656–662.

- S. Zhong, Y. Zhang, C. Lim, Tissue scaffolds for skin wound healing and dermal reconstruction, Wiley Interdiscip. Rev: Nanomed. Nanobiotechnol. 2 (5) (2010) 510–525.

- Adapting versatile polymers to improve surgical outcomes and patient recovery.

< http://polyganics.com/technology-platform > ,  2017  (accessed  03/10/2017).

- P. Schexnailder, G. Schmidt, Nanocomposite polymer hydrogels, Colloid Polym. Sci. 287 (1) (2009) 1–11.

- A.H. Peter Dubruel; Sandra VanVlierberghe, Hugues VanDenBergen, Patrice Roose,

Dirk Bontinck, Novel Urethane Based Materials, Derivatives, Methods of their Preparation and Uses, (2016).

- J. Van Hoorick, A. Ovsianikov, H. Declerq, M. Cornelissen, J. Van Erps,

H. Thienpont, P. Dubruel, S. Van Vlierberghe, Additive Manufacturing of 3D Gelatin Scaffolds: Direct Versus Indirect Printing, 10th World Biomaterials Congress,

Frontiers, (2016).

- J.I. Goldstein, Scanning Electron Microscopy and X-Ray Microanalysis, 3rd ed., Kluwer Academic/Plenum Publishers, New York, 2003.

- J. Van Hoorick, P. Gruber, M. Markovic, M. Tromayer, J.r. Van Erps, H. Thienpont,

R. Liska, A. Ovsianikov, P. Dubruel, S. Van Vlierberghe, Cross-linkable gelatins with

superior mechanical properties through carboxylic acid modification: increasing the two-photon polymerization potential, Biomacromolecules 18 (10) (2017)

3260–3272.

- I. Mironi-Harpaz, D.Y. Wang, S. Venkatraman, D. Seliktar, Photopolymerization of cell-encapsulating hydrogels: crosslinking efficiency versus cytotoxicity, Acta Biomater. 8 (5) (2012) 1838–1848.

- F. Ganji, F.S. Vasheghani, F.E. Vasheghani, Theoretical Description Of Hydrogel

Swelling: A Review, (2010).

- T. Billiet, B.V. Gasse, E. Gevaert, M. Cornelissen, J.C. Martins, P. Dubruel, Quantitative contrasts in the photopolymerization of acrylamide and methacryla-

mide-functionalized gelatin hydrogel building blocks, Macromol. Biosci. 13 (11) (2013) 1531–1545.

- S. Lin, N. Sangaj, T. Razafiarison, C. Zhang, S. Varghese, Influence of physical properties of biomaterials on cellular behavior, Pharm. Res. 28 (6) (2011)

1422–1430.

- S. Van Vlierberghe, P. Dubruel, E. Lippens, M. Cornelissen, E. Schacht, Correlation between cryogenic parameters and physico-chemical properties of porous gelatin cryogels, J. Biomater. Sci. Polym. Ed. 20 (10) (2009) 1417–1438.

- K.Y. Lee, K.H. Bouhadir, D.J. Mooney, Controlled degradation of hydrogels using

multi-functional cross-linking molecules, Biomaterials 25 (13) (2004) 2461–2466.

- B.V. Slaughter, S.S. Khurshid, O.Z. Fisher, A. Khademhosseini, N.A. Peppas, Hydrogels in regenerative medicine, Adv. Mater. 21 (32−33) (2009) 3307–3329.

- J. Mark, P. Flory, The configuration of the polyoxyethylene chain, J. Am. Chem. Soc. 87 (7) (1965) 1415–1423.

- D. Pezzoli, E. Cauli, P. Chevallier, S. Fare, D. Mantovani, Biomimetic coating of cross-linked gelatin to improve mechanical and biological properties of electrospun

PET: A promising approach for small caliber vascular graft applications, J. Biomed.

Mater. Res. Part A 105 (9) (2017) 2405–2415.

- S. Dahms, H. Piechota, R. Dahiya, T. Lue, E. Tanagho, Composition and bio-

mechanical properties of the bladder acellular matrix graft: comparative analysis in rat, pig and human, Br. J. Urol. 82 (1998) 411–419.

- A. Hasan, K. Ragaert, W. Swieszkowski, Š. Selimović, A. Paul, G. Camci-Unal,

M.R. Mofrad, A. Khademhosseini, Biomechanical properties of native and tissue engineered heart valve constructs, J. Biomech. 47 (9) (2014) 1949–1963.

- S. Pal, Mechanical Properties of Biological Materials, Design of Artificial Human Joints & Organs, Springer, 2014, pp. 23–40.

- A. Houben, Intelligent Hydrogel Design: towards more Performing Hydrogel Processing. PhD, in: UGent (Ed.) 2017.

- C.-C. Lin, A. Raza, H. Shih, PEG hydrogels formed by thiol-ene photo-click chem-

istry and their effect on the formation and recovery of insulin-secreting cell spheroids, Biomaterials 32 (36) (2011) 9685–9695.

- A.S. Sawhney, C.P. Pathak, J.A. Hubbell, Bioerodible hydrogels based on photo- polymerized poly (ethylene glycol)-co-poly (alpha.-hydroxy acid) diacrylate mac-

romers, Macromolecules 26 (4) (1993) 581–587.

- D. Snoeck, D. Schaubroeck, P. Dubruel, N. De Belie, Effect of high amounts of su- perabsorbent polymers and additional water on the workability, microstructure and

strength of mortars with a water-to-cement ratio of 0.50, Constr. Build. Mater. 72 (0) (2014) 148–157.

- R.D. Hancock, A.E. Martell, Ligand design for selective complexation of metal ions in aqueous solution, Chem. Rev. 89 (8) (1989) 1875–1914.

- B.-S. Chiou, S.R. Raghavan, S.A. Khan, Effect of colloidal fillers on the cross-linking

of a UV-curable polymer: gel point rheology and the Winter− Chambon criterion, Macromolecules 34 (13) (2001) 4526–4533.

- R. Lapasin, M. Abrami, M. Grassi, U. Šebenik, Rheology of Laponite-scleroglucan hydrogels, Carbohydr. Polym. 168 (2017) 290–300.

- K.A. Aamer, H. Sardinha, S.R. Bhatia, G.N. Tew, Rheological studies of PLLA–PEO–PLLA triblock copolymer hydrogels, Biomaterials 25 (6) (2004)

1087–1093.

- M.J. Bof, V.C. Bordagaray, D.E. Locaso, M.A. García, Chitosan molecular weight effect on starch-composite film properties, Food Hydrocoll. 51 (2015) 281–294.

- A.K. Gaharwar, R.K. Avery, A. Assmann, A. Paul, G.H. McKinley,

A. Khademhosseini, B.D. Olsen, Shear-thinning nanocomposite hydrogels for the treatment of hemorrhage, ACS Nano 8 (10) (2014) 9833–9842.

- A. Pei, J.-M. Malho, J. Ruokolainen, Q. Zhou, L.A. Berglund, Strong Nanocomposite reinforcement effects in polyurethane elastomer with low volume fraction of cel-

lulose nanocrystals, Macromolecules 44 (11) (2011) 4422–4427.

- M. Gasik, A. Gantar, S. Novak, Viscoelastic behaviour of hydrogel-based composites

for tissue engineering under mechanical load, Biomed. Mater. 12 (2) (2017) 025004.

- C. Loy, D. Pezzoli, G. Candiani, D. Mantovani, A cost-effective culture system for the

in vitro assembly, maturation, and stimulation of advanced multilayered multi- culture tubular tissue models, Biotechnol. J. 13 (1) (2017).

- N. Bono, S. Meghezi, M. Soncini, M. Piola, D. Mantovani, G.B. Fiore, A dual-mode bioreactor system for tissue engineered vascular models, Ann. Biomed. Eng. 45 (6)

(2017) 1496–1510.

- P.J. Photos, L. Bacakova, B. Discher, F.S. Bates, D.E. Discher, Polymer vesicles in

vivo: correlations with PEG molecular weight, J. Control. Release 90 (3) (2003) 323–334.

- K. Yue, G. Trujillo-de Santiago, M.M. Alvarez, A. Tamayol, N. Annabi,

A. Khademhosseini, Synthesis, properties, and biomedical applications of gelatin methacryloyl (GelMA) hydrogels, Biomaterials 73 (2015) 254–271.

- S. Van Vlierberghe, E. Vanderleyden, V. Boterberg, P. Dubruel, Gelatin functiona- lization of biomaterial surfaces: strategies for immobilization and visualization,

Polymers 3(1) (2011) 114.

- P. Dubruel, R. Unger, S. Van Vlierberghe, V. Cnudde, P.J.S. Jacobs, E. Schacht,

C.J. Kirkpatrick, Porous gelatin hydrogels: 2. In vitro cell interaction study, Biomacromolecules 8 (2) (2007) 338–344.

- W. Schuurman, P.A. Levett, M.W. Pot, P.R. van Weeren, W.J. Dhert,

D.W. Hutmacher, F.P. Melchels, T.J. Klein, J. Malda, Gelatin-methacrylamide hy- drogels as potential biomaterials for fabrication of tissue-engineered cartilage

constructs, Macromol. Biosci. 13 (5) (2013) 551–561.

- K. Hölzl, S. Lin, L. Tytgat, S. Van Vlierberghe, L. Gu, A. Ovsianikov, Bioink prop- erties before, during and after 3D bioprinting, Biofabrication 8 (3) (2016) 032002.

- E. Wischerhoff, K. Uhlig, A. Lankenau, H.G. Börner, A. Laschewsky, C. Duschl,

J.F. Lutz, Controlled cell adhesion on PEG-based switchable surfaces, Angew. Chem. Int. Ed. 47 (30) (2008) 5666–5668.

- D.A. Brafman, C.W. Chang, A. Fernandez, K. Willert, S. Varghese, S. Chien, Long- term human pluripotent stem cell self-renewal on synthetic polymer surfaces,

Biomaterials 31 (34) (2010) 9135–9144.

- J.K. Kutty, E. Cho, J. Soo Lee, N.R. Vyavahare, K. Webb, The effect of hyaluronic acid incorporation on fibroblast spreading and proliferation within PEG-diacrylate based semi-interpenetrating networks, Biomaterials 28 (33) (2007) 4928–4938.

- S.A. Bhakta, E. Evans, T.E. Benavidez, C.D. Garcia, Protein adsorption onto nano-

materials for the development of biosensors and analytical devices: a review, Anal. Chim. Acta 872 (2015) 7–25.

- R.A. Freitas, Nanomedicine, Volume I: Basic Capabilities, Landes Bioscience,

Georgetown, TX (1999).

- R. Jayakumar, M. Prabaharan, P.S. Kumar, S. Nair, H. Tamura, Biomaterials based

on chitin and chitosan in wound dressing applications, Biotechnol. Adv. 29 (3) (2011) 322–337.

- E.T. Anthony, M. Syed, S. Myers, G. Moir, H. Navsaria, The development of novel dermal matrices for cutaneous wound repair, Drug Discov. Today: Ther. Strateg. 3

(1) (2006) 81–86.

- G.D. Mogoşanu, A.M. Grumezescu, Natural and synthetic polymers for wounds and burns dressing, Int. J. Pharm. 463 (2) (2014) 127–136.