Supporting Information

Local Enhancement of Dopant Diffusion from Polycrystalline Silicon Passivating Contacts

Meriç Fırata,b,*, Lennaert Woutersb, Pieter Lagrainb, Felix Haasec, Jana-Isabelle Polzind, Aditya Chaudharye, Gizem Nogayf, Thibaut Desruesg, Jan Krügenerh, Robby Peibstc,h, Loic Tousb, Hariharsudan Sivaramakrishnan Radhakrishnanb, Jef Poortmansa,b,i

aKU Leuven, Department of Electrical Engineering, Kasteelpark Arenberg 10, 3001 Leuven, Belgium

bImec (Partner in EnergyVille), Kapeldreef 75, 3001 Leuven, Belgium

cISFH, Am Ohrberg 1, 31860, Emmerthal, Germany

dFraunhofer ISE, Heidenhofstraße 2, 79110, Freiburg, Germany

eISC-Konstanz, Rudolf-Diesel-Straße 15, 78467 Konstanz, Germany

fCSEM, Rue Jacquet-Droz 1, 2002 Neuchâtel, Switzerland

gUniversité Grenoble Alpes, CEA, LITEN, DTS, LPA, F-73370 Le Bourget-du-Lac, France

hLeibniz University Hannover, Institute of Electronic Materials and Devices, Schneiderberg 32, 30167 Hannover, Germany

iHasselt University, Campus Diepenbeek, Agoralaan Gebouw D, 3590 Diepenbeek, Belgium

*Corresponding author: meric.firat@student.kuleuven.be

## Additional Sample Design and Process Parameters

The samples prepared for the scanning spreading resistance microscopy (SSRM) measurements share a similar structure but still differ in various sample design and process parameters. The most relevant parameters for the process of dopant diffusion from polycrystalline silicon (poly-Si) passivating contacts into the underlying substrate are shown in Table 1, in the main body of the paper. Further parameters which are considered less significant for dopant distribution are summarized below, in Table S1. These parameters are (i) substrate parameters such as the wafer resistivity, the type of dopant in the wafer, and the wafer fabrication method, (ii) the Si film growth method, (iii) the Si film thickness (tSi), (iv) the method used for doping the Si film, and (v) the firing set peak temperature (Tf,p). We would like to note that the firing process was applied only to some of the samples, which all underwent silicon nitride deposition prior to firing.

Table S1. The less relevant design and process parameters of the samples used in this work. The symbols and abbreviations stand for the following phrases: P: Phosphorus, B: Boron, Cz: Czochralski, FZ: Float Zone, Si: Silicon, LPCVD: Low Pressure Chemical Vapor Deposition, PECVD: Plasma Enhanced Chemical Vapor Deposition, tSi: Si film thickness, PIII: Plasma-Immersion Ion Implantation, Tf,p: firing set peak temperature.

| Name | Substrate Properties (Resistivity, Dopant, Fabrication Method) | Si Growth Method | tSi | Si Doping Method | Tf,p |
| --- | --- | --- | --- | --- | --- |
| Imec-A | 2.8 Ω∙cm, P, Cz | LPCVD | 150 nm | In situ | No firing |
| Imec-B | 2.8 Ω∙cm, P, Cz | LPCVD | 150 nm | In situ | No firing |
| Imec-C | 2.8 Ω∙cm, P, Cz | LPCVD | 150 nm | In situ | No firing |
| Imec-D | 2.1 Ω∙cm, P, Cz | LPCVD | 150 nm | In situ | No firing |
| CEA | 2.3 Ω∙cm, P, Cz | LPCVD | 150 nm | Ex situ (PIII) | 700°C |
| ISE | 1 Ω∙cm, P, FZ | PECVD | 40 nm | In situ | No firing |
| ISFH-A | 1.3 Ω∙cm, B, FZ | LPCVD | 220 nm | Ex situ (Ion implantation) | No firing |
| ISFH-B | 1.3 Ω∙cm, B, FZ | LPCVD | 220 nm | Ex situ (Ion implantation) | No firing |
| ISFH-C | 1 Ω∙cm, P, Cz | LPCVD | 200 nm | In situ | 810°C |
| ISC | 3.7 Ω∙cm, P, Cz | LPCVD | 150 nm | In situ | 790°C |

## Details of Contact Resistivity Measurements

Contact resistivity (ρc) of the passivating contacts on the samples used for the scanning spreading resistance microscopy (SSRM) measurements are shown in Table 2, in the main body of the manuscript. Most of these values were measured by the transfer length method (TLM) and reported in various references cited in Table 2, where further details regarding the extraction of ρc can be found. Nevertheless, an overview of the measurement details is also provided in Table S2 since these can influence the data in Table 2. Table S2 shows (i) by which metallization techniques the contact pads on the TLM samples were fabricated, and (ii) whether the poly-Si film between the contact pads was removed for accounting for the impact of carrier transport through the interfacial SiOx film in the ρc measurement.

Table S2. Details of contact resistivity (ρc) measurements performed on each sample by the transfer length method (TLM).

| Name | Metallization Method | Poly-Si Removal between TLM Pads |
| --- | --- | --- |
| Imec-A | Electron-beam evaporation of Ti/Al | Yes |
| Imec-B | Electron-beam evaporation of Ti/Al | Yes |
| Imec-C | Electron-beam evaporation of Ti/Al | Yes |
| Imec-D | Electron-beam evaporation of Ti/Al | Yes |
| CEA (No ρc measurement) | - | - |
| ISE | Thermal evaporation of Ti/Pd/Ag | Yes |
| ISFH-A | Thermal evaporation of Al | Yes |
| ISFH-B | Thermal evaporation of Al | Yes |
| ISFH-C | Fire-through screen-printing of Ag paste | No |
| ISC | Fire-through screen-printing of Ag paste | No |